# GUIDELINES FOR USING

POLISHING SWABS

To avoid scratching the surface, do not wear watches, rings, or bracelets.  Long fingernails should be covered with gloves.

Keep MICRO-MESH( swabs clean; contamination can cause scratches.  When finished using, rinse MICRO-MESH( swabs, air dry, and return them to their original packaging.  MICRO-MESH( is reusable!

Use only 100% cotton flannel for wiping.  Keep it clean, wash in warm soapy water, rinse, dry and return to the kit box.

Pressure Should be Light.  Remember the cushioned abrasive cuts with the abrasive crystal tips.  The sharp cutting edges are floating on a resilient matrix.  Extreme pressure pushes the tips back into the matrix rendering them ineffective and resulting in surface smearing, burning, and possible orange peel and distortion.

Unacceptable Cleaning and Maintenance Materials:

Paper towels or other paper products

Shop towels or synthetic fiber fabrics

Commercial window cleaners

Any product containing ammonia or solvents or alcohol

Clean the Work Surface between each step, especially in cracks and crevices.  Flush surface several times with clean water to remove dust and dirt before touching it with anything. Clean abraded particles from the work piece by rinsing and then dry and inspect.

Inspect the Work Piece between steps with a bright light to ensure you are removing the previous scratch pattern before continuing on. Using MICRO-MESH® with Water and a few drops of detergent will generally result in a less effort having to be used and a slightly better finish.  Only use enough water to provide lubricity to the surface, but not so much that poor contact is made with the work piece.

DO NOT wear out one of the meshes by trying to make it do too much work on your first step.  If your estimated damage is not readily removed, go immediately to the next coarser mesh.  Removing the initial damage with the sandpaper series will take up 85% of the restoral time.  The MICRO-MESH series and the buffing procedures will take as little as 15% of the time. DO NOT skip steps.

Work an area slightly larger with each step to blend.  Working one small area on a highly curved section could create flat spots or distortion.

IMPORTANT NOTICE: Micro-Surface Finishing Products, Inc. (“Micro”) MAKES NO WARRANTIES, EXPRESS OR IMPLIED, INCLUDING, BUT NOT LIMITED TO, ANY IMPLIED WARRANTIES OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE.  User is responsible for determining whether this product is fit for a particular purpose and suitable for user’s method of application.

LIMITATION OF REMEDIES AND LIABILITY:  If this product is proved to be defective, THE EXCLUSIVE REMEDY, AT MICRO’S OPTION, SHALL BE TO REFUND THE PURCHASE PRICE OF OR TO REPAIR OR REPLACE THE DEFECTIVE PRODUCT.  Micro shall not otherwise be liable for loss or damages, whether direct, indirect, special, incidental, or consequential, regardless of the legal theory asserted, including negligence, warranty or strict liability.

06/20/09

Guidelines for Using Swabs